Rheological characterization of fish skin gelatin and κ-carrageenan mixtures

CJ Marsal, F.Badii and N. Howell

Department of Nutritional Sciences, Faculty of Health and Medical Sciences, School of Biosciences and Medicine, University of Surrey, Guildford, Surrey, UK GU2 7XH

Marine gelatin has a broad range of applications in both the food and pharmaceutical industries as it is as a hydrocolloid with exceptional texture characteristics. Fish and animal skins which are by-products of the meat and fish processing industries, can be used for extracting gelatin, that has important nutritional and functional properties1. The skin of warm-water fish such as tilapia is a potential source for gelatin that can be used in products requiring high gel strength. The aim of this study was to investigate the interaction of tilapia fish skin gelatin with к (kappa)-carrageenan, a common stabiliser used in dairy products, in terms of the rheological properties. Tilapia gelatin (TG) was extracted from the skin of tilapia (Oreochromis niloticus). Aqueous solutions were prepared with 5% (w/v) TG and 0.25%, 0.50% or 0.75% (w/v) κ-carrageenan (CG) and subjected to small and large deformation rheological tests. The gelling temperatures of 5% TG + 0.25% CG, 5% TG + 0.50% CG and 5% TG + 0.75% CG were  21.7°C,  28.7°C and 38.9°C respectively, which were higher than for 10% TG alone (19.9°C). Thus an increase in the к-carrageenan concentration resulted in a higher gelling temperature of the mixture. The mixtures of tilapia gelatin containing increasing concentrations of κ-carrageenan (0.25, 0.5 and 0.75% CG) resulted in high elastic modulus (G’) values; 33.0 Pa, 134.5 Pa and 627.4 Pa respectively compared to 20.5 Pa for tilapia gelatin alone. The gel melting behaviour was explained as a two- step process, which is the conformational change of helices involved in the network junction zones followed by the melting of aggregates 2. The complexes of fish gelatin and к- carrageenan at 60°C were probably stabilised by electrostatic interactions3. The Bloom strength of gelatin at 6.67% (w/v) in water was 218.2 + 10.4 whereas the commercial samples had Bloom values of 78.4 + 0.6 and 107.7 + 1.0 respectively.  In conclusion, an increase in κ- carrageenan concentration in the mixture resulted in better gelling properties. The formation of gelatin-к-carrageenan complexes and concentration of free gelatin in an aqueous phase determine the stability and the rheological properties. Thus, an increase in the к-carrageenan/ gelatin (w/w) ratio led to increased gelatin-к-carrageenan complexes and higher storage modulus values.

References:

1	Badii. F & Howell.N.K. (2006). Fish gelatin: Structure, gelling properties and interaction with egg albumen proteins. Food Hydrocolloids, 20, 630-640.

2	Mangione, M.R. et al. (2003). Thermoreversible gelation of к- Carrageenan: relation between conformational transition and aggregation. Biophysical Chemistry, 104, 92-105.

3	Haug, I. et al. (2004). Physical behaviour of fish gelatin-к-carrageenan mixtures. Carbohydrate Polymers, 56, 11-19.