Rheological properties of a polysaccharide isolated from Treculia africana fruit pulp

Louis M. Nwokocha1,* and Peter A. Williams2

1Department of Chemistry, University of Ibadan, Ibadan, Nigeria

2Center for Water Soluble Polymers, Glyndwr University, Wrexham,

North Wales LL 11 2AW, UK

*Abstract presenting: (lm.nwokocha@mail.ui.edu.ng)

Abstract

A water soluble polysaccharide was isolated from the Treculia africana fruit pulp. It had an intrinsic viscosity of 183±0.14 mL/g, weight average molar mass of 1.62 x 106 g/mol and polydispersity index of 3.8. The log- log plot of RMS radius (Rg) versus molar mass (MW) had an exponent of 0.54 indicating the polysaccharide solution contained random coil polymers. The shear viscosity-shear rate profiles showed the polymer solutions were characterized by low viscosity. The activation energy of viscous flow determined at polymer concentrations 25% (17.67 kJ/mol) and 32% (18.48 kJ/mol) showed concentration dependence. The mechanical spectra showed the polysaccharide concentration at 32% was purely viscous with G” >> G’ and both moduli showing strong dependence on frequency.